## Slide 1
Bedzyk Research Group
X-ray Interface Science
INTERFACIAL SCIENCE
by its very nature brings together a
diverse interests in oxide films, catalysis,
semiconductors, nano-science, bio-membranes,
surface physics, corrosion, and electrochemistry.
One of many grand challenges in the overall interdisciplinary field of interfacial science is the need
to observe and control the assembly of atoms,
molecules and supported nanoparticles at well-defined interfaces in complex environments.
With atomic resolution and high penetrating power,
we are developing and applying sophisticated
in situ X-ray methods to meet
these challenges.
From Bottom Left:
Kurinji, Liane, Professor Michael J. Bedzyk, Bor-Rong, Stephanie, Janak, Xueting, Changrui, Allison, Xiao, Guena, Weishen, Sumit, Boris, Li, Gavin
Small Angle X-ray
Scattering (SAXS)
X-Ray Absorption
Fine Structure
(XAFS)
X-Ray Reflective (XRR)
Wide Angle X-ray
Scatter (WAXS)
X-Ray Standing Wave (XSW)
E - Ebinding
Energy (keV)
f’
f’’
0
Rb+
Anomalous Small Angle X-Ray Scattering (ASAXS)
Determines the ion distribution around DNA-protein particles
Through probing the scattering pattern at energies below and at the Rb K absorption edge, the ion distribution around the proteins can be extracted. This has important implications on the extent of the DNA shell, the higher melting temperatures associated with the constructs, and resistance to enzymatic degradation.
SAXS probes electrolyte-mediated assembly of SNA-Au NPs
XAFS Elucidates the Role of Trace Ag in Au Nanorod Growth
Gas-like
FCC
Disordered
FCC
Gas-like
Glass-like
Is
Electrolyte-mediated assembly
SH-TTTT….TTTT
40 bases (T40)
9 nm
Au
ss-DNA-AuNP (S-SNA)
DNA-Au NPs can assemble into organized structures in the absence of Watson-Crick base pairing using electrostatics alone in high ionic strength conditions. At lower ionic strength, the particles show no inter-particle interaction, or a “gas-like” phase. As the ionic strength is increased, the DNA-Au NPs assemble into a close-packed FCC structure. As the ionic strength is increased to even higher values, the structure loses its order, and a glass-like phase is observed, which is most accurately modeled as hexagonal random packing.
Our Approach: Create “timeline” of reaction
highly anisotropic rods formed by 12 minutes in reaction time
reaction quenched using BSPP (bis(p-sulfanatophenyl)phenyl-phosphine)
global structure
local structure
oxidation state
8 minutes
length = 9.6 nm
diameter = 6.3 nm
aspect ratio = 1.5
12 minutes
length = 23 nm
diameter =6.3 nm
aspect ratio = 3.6
45 minutes
length = 51 nm
diameter = 14 nm
aspect ratio = 3.7
120 minutes
length = 54 nm
diameter = 15 nm
aspect ratio = 3.7
Electron Microscopy (EM)
X-Ray Fluorescence (XRF)
Extended X-Ray Absorption Fine Structure (EXAFS)
X-Ray Absorption Near Edge Structure (XANES)
100 nm
200 nm
200 nm
200 nm
Reaction Time
XRF
EXAFS
Ag deposits early in the reaction on the nanorod surface and incorporates into bulk as the reaction progresses. When a high percentage of {110} surface atoms are Ag, the length growth rate exceeds the diameter growth rate. As Ag incorporates into bulk and is not on the surface, the length and diameter growth rates are equal by reaction completion.
Molecular assembly of amphiphilic binary mixtures:
Solution X-ray scattering studies
2-D intermolecular packing (2D hexagonal, rectangular-C, etc.) of amphiphilic binary mixtures is highly dependent on parameters like pH and lipid tail length, which can control the overall mesoscopic morphology of assembly: closed faceted vesicles or planar bilayer ribbons, by changing the local crystalline order of the amphiphile tails.
Pd nanoparticles supported on SrTiO3 nanocuboids
The morphology and catalytic performance of atomic layer deposition (ALD) grown Pd nanoparticle supported on SrTiO3 nanocuboids with well-defined (001) surfaces that are either a TiO2- or SrO- terminated surface.
The chemical state and local structure of Pd nanoparticle are measured by X-ray techniques
Local structure measured by extended X-ay absorption fine structure (EXAFS)
Chemical state measured by X-ay absorption near edge structure (XANES)
STO
Pd
STO
Pd
Energy Materials
In situ X-ray Reflectivity (XRR): monitors thin film material morphology changes in special designed transmission cell.
Ge/Ti multi-layer
Ga is seen to increases the crystallization temperature
Samples were annealed for 1 hour in 25°C increments. Glancing incidence X-ray diffraction monitors the transition from amorphous to crystalline film
Effects of Ga on a-IGO crystallization
EXAFS Samples: | N | R: Ga-O (Å)
c-Ga2O3 (model) | 5 | 1.85, 2.01
a-Ga-O | 4.3 | 1.88
Ga doped a-In-O | 3.9 | 1.88
Ga-O bond distance is consistently between that of 4-fold coordinate Ga and 6-fold coordinate Ga. Ga’s ability to increase crystallization temperature is attributed to presence of 4-fold sites.
By using X-ray scattering, we can detect the structure of lipid assembly on multiple length scales, and study their phase transition behavior.
Monitoring Ligand Substitution on PbS nanoparticles
- x1000 expected increase in
hoping rate
- No conductivity across ~1cm
6 Å
3 Å
Oleate
Thiocyanate
20 Å
2.8 Å
PbS nanoparticles undergo quantum confinement in the infrared at small size-scales, which make them candidates for infrared LEDs and photo-detectors. Transport within nanoparticle films occurs electron hoping between neighboring nanoparticles. Conduction can be tailored by reducing particle to particle distance. One way to achieve this is by ligand substitution, wherein the native Oleate ligands are replaced with shorted Thiocyanate ligands reducing the gap space by 3 Angstroms and increasing hoping rate by several orders of magnitude. However, this process degrades the film which can be seen in SEM from crack formation and in GISAXS by the reduction of 2nd and 3rd order peak intensity. The result is that the film is none conductive over long length scales.
Self-Assembled Nano-Dielectrics (SAND)
Ultra thin high-k dielectric materials needed for low mobility organic semiconductor.
= Br -
Alternating inorganic/organic layered structures
Low leakage current, high capacitance, solutions-process method, low deposition T
Long-period XSW generated by layered Synthetic Microstructure (Si/Mo multilayers).
Sensitive to heavy elements
Capable of probing elemental position w/ sub-nanometer resolution.
Amorphous indium oxide has higher mobility than other TFT semiconductoring layer materials however, it needs to be structurally stabilized
X-Ray Studies of Solar Cells
GIWAXS of Lead perovskite showing texturing and residual PbI2 (smallest ring)
Four homologue dyes for Solar cells
X-ray Reflectivity (XRR) curves for dye monolayers
Au
Spiro-OMeTAD
Compact TiO2
FTO
CH3NH3PbI3-xClx
+ TiO2
Density profiles of dyes on thin TiO2 deduced from XRR
With P. Stair (Chemistry), K. Poeppelmeier (Chemistry), and L. Marks (MatSci) groups