## Slide 1
X-Ray Materials Science
Michael Bedzyk
Materials Research Science and Engineering Center (MRSEC)
Institute for Catalysis in Energy Processes (ICEP)
Center for Electrical Energy Storage (CEES)
Synchrotron Research Center (SRC)
Argonne Northwestern Solar Energy Research Center (ANSER)
Center for Hierarchical Materials Design (CHiMaD )
Funding: NSF, DoE, AirForce, NIST
X-rays: APS, NU X-ray Lab

## Slide 2
Bedzyk group:
Group breakdown: 2 postdocs, 10 PhD graduate students:
6 MSE,
3 Applied Physics
1 Physics & Astronomy
3 grads finishing next year

## Slide 3: Research Group Theme: X-Ray Interface Science
Organic/Inorganic Hybrid Interfaces
2D Materials
Oxide Supported Catalysts
Super Alloy Films MGI
Amorphous Oxide Semiconductors
Electrode-Electrolyte Interface
Molecular Assembly (Membranes & Fibers)
DNA-Nanoparticle Assembly
Si
SiO2

## Slide 4: Some X-ray Basics: Wave Property Structural Info λ = 0.1 to 10 Å wavelength E-M radiation X-rays scatter coherently from electrons Particle Property Compositional Info Eϒ = 1 to 100 keV energy Photo effect: Inner shell (K, L) ionization XRF : Decay of excited ion to ground state by characteristic XRF emission

## Slide 5
X-ray Vision
Advantage:
Weak interaction with matter
High penetrating power
In situ analysis
 Buried structures
Atomic-scale resolution
Problem:
Weak interaction with matter
 weak signal
Need very intense X-ray source

## Slide 7
Brightest X-ray Source in Western Hemisphere
= Advanced Photon Source
relativistic electrons pass thru periodic magnetic array
Undulator Device

## Slide 8
Grazing Incidence
Surface Sensitivity
X-ray Scattering Diffractometer at Advanced Photon Source

## Slide 9: Argonne National Laboratory
NU
ANL
ORD
NU-ANL Carpool
Funded by US Dept. of Energy Lab

## Slide 10: What a new student in the Bedzyk group might expect to be involved with while pursuing their PhD
Gain an expertise with general x-ray techniques and experimental design
Learn fundamental materials science/ chemistry/ physics/ biology relevant to the systems they are studying (interdisciplinary research)
Take measurements at the Advanced Photon Source
Understand atomic-scale structure and how it correlates with desirable materials properties

## Slide 11
Argonne collaborative projects
looking for 5 new grad students
3 with Nenad Markovic, MSD, JCESR
Electrode/Electrolyte Interface Structure & Properties
1 with Paul Fenter, CSE
Water-Solid Interactions
1 with Anand Bhattacharya, MSD & CNM
Digital Synthesis: Tailoring novel properties in complex oxides

## Slide 12
Energy Conversion and Storage Group
Exceptional group of students, postdoctoral fellows and young scientists
D. Strmcnik
N. Markovic
K-C Chang
P. Paulikas
H. You
The feature of surface electrochemistry
V. Stamenkovic
Looking for 3 new Graduate Students

## Slide 13
Revolutionize the science and technology of advanced alternative energy conversion and storage systems
Transportation
Storage
Vision
Legacies
Model
Commercial
A library of fundamental knowledge
A new paradigm for transformative science
Lifting the wall between water and organic EC systems
Energy Conversion and Storage Group: N. M. Markovic
Develop active, stable, selective and cost-effective materials
Fuel Cells
Electrolyzers
Batteries
Mission
H2
H2
O2
O2
CxHyO
CxHyO
2

## Slide 14
PHYSICAL
CHEMICAL
–– SYNTHESIZE
SYNTHESIS METHODS
Batteries
–– APPLY
–– UNDERSTAND
Theory/Modeling
Experiment
ACTIVITY, SELECTIVITY AND STABILITY MAPPING
CsOH
LiOH
KOH
Ru
Pt
Au
3
DOUBLE-LAYER-BY-DESIGN
ANIONS
CATIONS
SOLVENT
DESIGN
MATERIALS-BY-DESIGN
METALS
METAL OXIDES
OXIDES
Single
Crystals
Real
Nano
Model
Nano
UHV
FTIR
SXRD
STM/AFM
RAMAN
HRTEM
–– CHARACTERIZE
CHARACTERIZATION METHODS
Surface Science Approach
REAL SYSTEM
Pt
Fuel Cell  Electrolyzer

## Slide 15
Interfacial Processes Group
Chemical Sciences and Engineering Division, Argonne National Laboratory
Research Staff:
Paul Fenter
Senior Physicist,
Group Leader
Sang Soo Lee
Geochemist
Tim Fister
Physicist
Post-Doctoral Fellows:
Ke Yuan (Geochemist), Jonnathan Medina-Ramos (Electrochemist), Soojeong Kim (Chemist)
Jae Jin Kim (Materials Scientist), Zhenxing Feng (Materials Scientist),
Graduate Students:
Xiao Chen (Applied Physics, Northwestern University)
Erika Callagon (Earth and Environmental Sciences, University of Illinois, Chicago)

## Slide 16
Understanding Water-Solid Interactions: P. Fenter
Background: The interaction of water with solid surfaces is central to a wide range of systems and processes
- Corrosion, electrochemistry, ion separations, catalysis, biofouling, water purification.
Water is a very unusual material due to its hydrogen bonding network
- e.g., with a solid phase that is lower in density w/r to the liquid.
Interfacial Water at Solid Surfaces*:
Interfacial reactivity and wetting are controlled by interfacial hydration layers that are defined by the water hydrogen bonding (e.g., water-water vs. water-solid interactions).
*Fenter and Lee, MRS Bulletin, December 2014.
Water contact angles (graphene/SiC)**:
ZLG: “zero layer graphene; the epitaxial buffer layer
BLG: “bilayer graphene”
**Zhou et al., Phys. Rev. B 85 035406 (2012)

## Slide 17
Super-Hydrophobic
Lotus leaf
NanoTex cloth
stain resistant clothing

## Slide 18
Goal: Developing a robust molecular-scale understanding the water organization at the solid-water interface.
X-ray reflectivity at the water-solid interface:
Guiding Questions:
How does water organize at interfaces?
vertical and lateral water organization.
direct visualization of hydrogen bonding network.
Can we independently test and validate the experimentally determined structures with high level computations
- Coordinated studies with parallel density functional theory via the MICCoM Center*
Example: vertical water structure at graphene:
**Midwest Integrated Center for Computational Materials
Understanding Water-Solid Interactions: P. Fenter
X-ray

## Slide 19
Stephen Wu (postdoc), Jason Hoffman (recent postdoc, @ Harvard), Anand Bhattacharya (PI)
John Pearson
(Sr. Engineer)
Prof. Brittany Nelson-Cheeseman, U. St. Thomas, MN
Prof. Ming Liu,
Xian Jiaotong U., China
Prof. Steve May,
MSE Drexel U., PA
Dr. Tiffany Santos,
Staff, HGST, CA
Postdoc Alumni
Digital Synthesis: tailoring novel properties in complex oxides
Anand Bhattacharya, anand@anl.gov
Notes: Our current team consists of postdoc Stephen Wu, Sr. engineer John Pearson and PI Anand Bhattacharya. Jason Hoffman, a recent postdoc, has moved on to Harvard as a research associate. We have had postdocs go through our program since 2007 – starting with Steve may who is now faculty at Drexel, Tiffany Santos who is now a Staff Scientist at HGST San Jose, Brittany Nelson Cheeseman who is now faculty at U. St. Thomas and Ming Liu, who joined the faculty at Xian Jiaotong University as part of the 1000 talents program.

## Slide 20
Digital Synthesis: tailoring novel properties in complex oxides
Explore
Magnetic structure; TN increases by 70 K
Nat. Mater. 8, 892 (2009).
Conceive
What is the role of cation disorder?
Discover
Canted magnetic state
PRL 107, 167202 (2011).
Synthesize
LaMnO3/SrMnO3
Create model materials systems with oxide-MBE
Anand Bhattacharya, anand@anl.gov
Notes: The complex oxides are some of the most promising and interesting materials for energy. Digital Synthesis is a way to tailor complex oxides with new and novel properties. So how does this work? In our program, the conception of a new ‘digital oxide’ begins with asking a simple question. For example, we have asked - what is the role of disorder in the properties of manganites? We can address this by synthesizing a model system like the one in this figure, with single unit cell precision. Next, we explore the structure and properties of this material. With the amazing tools available to us now, we can in fact find out where all the atoms are in our sample, what the bonds between them are doing, and how their spins are arranged. This, coupled with other measurements leads to new insights and discovery of novel properties. For example, we have shown that manganite superlattices made this way can have record high Neel temperatures. In the last review period, we realized a canted magnetic state that was predicted by deGennes in his seminal paper, and pointed out as one of the outstanding quests in the field of manganites in Elbio Dagotto’s book on the subject. This process repeats as we refine our questions and improve our understanding of these materials, and our ability to design new properties.

## Slide 21: Recent Highlight: Discovery of Paramagnetic Spin Seebeck Effect
Paramagnetic Spin Seebeck Effect, S. Wu, J. Pearson, A. Bhattacharya, Phys. Rev. Lett. 114, 186602 (2015) (Editor’s Suggestion);
Also first observation of Antiferromagnetic SSE (arXive 2015)
Notes: Notes: When a thermal gradient is applied across a ferromagnetic material, it can drive a spin current via the spin Seebeck effect. A few years ago, it was shown that this effect also works in ferromagnetic insulators where the charge degree of freedom is strongly gapped. Here, a ‘pure’ spin current results from a thermal imbalance in the population of magnons. In this work, we have shown that the spin Seebeck effect can also occur in paramagnetic insulators that nominally do not support magnons.
The result is surprising and also encouraging as it broadens the class of materials that may be used to generate spin currents, particularly at low temperatures. For example, in geometrically frustrated pyrochlore magnets that host spin ice and spin liquid ground states, the excitations can be quire unusual – such as magnetic monopoles and spinons. Coupling to these excitations and moving them around remains a challenge. Our results imply that we may be able create spin currents from these excitations using local thermal gradients, and detect them via the inverse spin Hall effect.
The technique to carry out this measurement was developed at Argonne (work published by the same team in APL and JAP in the past year), where a patterned Au wire about 10 microns wide was used to deliver the heat locally to the surface of the paramagnet. This results in a large out-of-plane thermal gradient near the surface that drives a spin current out of the underlying paramagnet. The spin current is detected using the inverse spin Hall effect in W or Pt layers on the surface of the paramagnet. The signal is quite large and comparable to what is observed in the more conventional YIG/Pt structures. Note that the Au heater wire and the detector layer are electrically isolated from each other.

## Slide 22
Recent Highlight: Tailoring bond lengths with electrostatics
“Polar cation ordering: A route to introducing > 10% bond strain into layered oxide films”, B. B. Nelson-Cheeseman, H. Zhou, P. V. Balachandran, G. Fabbris, J. Hoffman, D. Haskel, J. M. Rondinelli, A. Bhattacharya, Advanced Functional Materials 24 (2014)
Notes: By using a layer by layer synthesis approach, we are able to tailor artificial dipoles within a material. Here, this is done by layering LaO (+1), NiO2 (-1) and SrO (0) in a manner that produces a dipole within each formula unit of LaSrNiO4. This makes LaSrNiO4 a ‘polar’ metal. We observe a distortion of the NiO bond lengths along the c-xis (vertical direction on this slide) that are a resukt of the crsytal trying to compensate for the dipole that we have artificially introduced. This is a new approach to tailor bond lengths and thus the elctronic and magnetic properties of oxides.

## Slide 23
Argonne collaborative projects
looking for 5 new grad students
3 with Nenad Markovic, MSD, JCESR
Electrode/Electrolyte Interface Structure & Properties
www.msd.anl.gov/markovic
1 with Paul Fenter, CSE
Water-Solid Interactions
www.msd.anl.gov/fenter
1 with Anand Bhattacharya, MSD & CNM
Digital Synthesis: Tailoring novel properties in complex oxides
www.msd.anl.gov/bhattacharya
M. Bedzyk will arrange meetings both at NU and at ANL